## Slide 1
PrintPur Polyurethane Resins for Printing Inks
April 11th 2011
Notes: <number>

## Slide 2
<number>
Types of Polyurethane available
The PU in the ink has the role to make a polymeric film after the solvent evaporation.
The PU in the ink acts mainly as plasticiser of the binder (NC, PVB, PVC, etc..) because it isn’t able to form a non-tacky film by itself.
LOW MOLECULAR WEIGHT
(PRINTPUR LM SERIES)
HIGH MOLECULAR WEIGHT
(PRINTPUR HM SERIES)
Molecular weights < 20000
High solid content, from 70 to 100%
Molecular weights > 25000
Low solid content from 25 to 45%

## Slide 3
<number>
PrintPur LM Series
PrintPur LM | Isocyanate Type | Solvents | Solid Content | Remarks
401 | TDI | Ethanol | 75% | Star Product. General Purpose. Good Balance : Hardness / Softness
402 | TDI | Ethanol | 75% | High Flexibility. High Mechanical Resistance (Crinkle and Rub).
403 | TDI | Ethyl Acetate | 80% | Alkoxy terminated. High compatibility with solvents. If used in combination with other Printpur, it can improve the roller cleaning.
404 | MDI | Ethyl Acetate | 70% | Especially for Gravure. Very good Printability. High Water, Grease and Milk Resistance. Mono-solvent.
407 | TDI | Solventless | 100% | OH Functionalized. Especillay for pigment grinding (chips and bases) It can be used in combination with other PrintPur grades to increase the flexibility of the system.

## Slide 4
<number>
PrintPur HM: Standard Grades
PrintPur HM | Isocyanate Type | Solvents | Solid Content | Remarks
424 | Semi- Aliphatic | Ethanol / Ethyl acetate (80/20) | 45 % | General purpose. Good softness/hardness balance providing good Printability and Bonding strength in the most common laminate systems.
416 | Semi- Aliphatic | Ethanol / Ethyl acetate (80/20) | 42 % | Softer Version of PrintPur HM 424 to improve the Bonding Strength
423 | Semi- Aliphatic | Ethanol / Ethyl acetate (80/20) | 42 % | High polar functional groups. Especially designed for pigment grinding. Provides hard film.
412 | Pure Aliphatic | Isopropanol / Ethyl Acetate (40/60) | 43 % | Poly(Ester-Urethane). High adhesion and Bonding Strength in several applications and especially with PET substrates
414 | Pure Aliphatic | Ethyl acetate | 30 % | Poly(Ester-Urethane). High adhesion and Bonding Strength in several applications and especially with PET substrates. Suitable for Mono-solvent and for NC free Retortable Inks

## Slide 5
<number>
PrintPur HM: Special Grades
PrintPur HM | Isocyanate Type | Solvents | Solid Content | Amine N. mgKOH /g | Remarks
408 | Pure Aliphatic | Ethanol / Ethyl acetate (50/50) | 25 % | 0 | Very hard film. High adhesion and Bonding strength with various substrates. Suitable as NC or PVB Plasticizers.
428 | Pure Aliphatic | nPropanol / nPropyl Acetate (30/70) | 35 % | 5 | Very hard film. High adhesion and Bonding strength with various substrates High Bonding strength also in Extrusion lamination. Suitable as NC or PVB Plasticizers.
422 | Semi- Aliphatic | Ethanol / Ethyl acetate (10/90) | 46 % | 4 | New Generation Poly(Urethane) Resin. High Adhesion on different substrates and Adhesion on PP without Promoters
427 EXP | Aliphatic | Ethanol / Ethyl acetate (10/90) | 43 % | 0 | Pure Aliphatic Poly(urethane) for retorting Applications. Low yellowing Tendency and High Stability in Thermal Processes.

## Slide 6
<number>
PrintPur Series at Low Ethanol Content
PrintPur | Isocyanate Type | Solvents | Solid Content | Remarks
401 EA | TDI | Ethanol < 2% Ethyl Acetate | 75% | Star Product.General Purpose. Good Balance : Hardness / Softness
425 | Semi- Aliphatic | Ethanol < 12% Ethyl acetate | 43 % | High polar functional groups. Especially designed for pigment grinding. Provides hard film.