## Slide 1
PRINTESTER Polyester Resins for Liquid Packaging Inks
February 15th 2010
Notes: <number>

## Slide 2
<number>
Types of Polyesters available
Flexible polymer to plasticize PVC, but also suitable for PVAc and NC.
Flexible polymer used for the formulation of solvent based varnishes.
Polyesters for 2K Systems
(PrintEster 101, PrintEster 401)
Plasticizers
(PrintEster 102 and 102 75AE)
High solid content, from 70 to 80%
Solventless, or 75% in Ethyl Acetate

## Slide 3
<number>
PRINTESTER Polymers (1/2)
Print Ester | Type / Solvent | Solid Content | MW (g.mol-1) | Visco. (Brookfield) dPa.s | Acid Value (mg KOH/g) | Hydroxy Number (mg KOH/g) | Application
401 | Aromatic in Ethyl Acetate | 71% | 8000 | 9,5 ± 2 | 17,5 | 194 – 242 | To be used in general 2K OPV and Inks in combination with Isocyanates. Provides excellent gloss, high chemical resistance and fast-tack-free.
101 | Aliphatic in Ethyl Acetate | 80% | 8000 | 7,0 ± 2 | 4,0 | 200 - 220 | Polyester to be used in general 2K OPV in combination with Isocyanates. Especially recommended for white varnishes due to its low-yellowing.

## Slide 4: Additional information on Polyester for 2K
<number>
Reactivity :
  OH number = 220mg KOH / g
Solubility in Ethyl acetate (due to its low MW)
Good properties of the film after curing :
  High gloss
  High resistances
  Fast tack-free
  Good adhesion on plastics and metallic substrates

## Slide 5
<number>
PRINTESTER POLYESTER Plasticizers (2/2)
Print Ester | Type / Solvent | Solid Content | MW (g.mol-1) | Visco. (Brookfield) dPa.s | Acid Value (mg KOH/g) | Hydroxy Number (mg KOH/g) | Application
102 | Aliphatic | 100% | 28000 | 10,5 ± 3,5 (T=80°C) | < 5,5 | 15 | Plasticizer for PVC systems. High performance and adhesion on PET and plastic substrates.
102 75 AE | Aliphatic in Ethyl Acetate | 75% | 28000 | 35,0 ± 6 | < 10,0 | <35 |